Photographic developing anti-etching ink (XR-7000)

XR-7000 is the introduction of Japanese technology developed for one-component UV contact exposure, alkali development, anti-etching, plating resistance, antioxidant ink. Widely used in metal utensils, molds, flower roll, crafts, plate, stainless steel mesh, high-precision electronic hardware components of the etching. Imaging and high anti-etching ability, performance and stability. Also for the production of single, double and multilayer circuit board precision,. Acid etching solution and resistance to copper, tin, lead and nickel-gold plating solution, its performance is more superior than the dry。

Operational processes and technical parameters：

Substrate pre-treatment

Acid treatment and brushing with the same general pre-treatment

Coated cloth

Pre-dry

Stir, full plate printing, plating 120-150 mesh, etched with a 200-250    mesh screen, for 15 minutes after printing

Exposure

75 ~ 85 ℃ ,10-20 minutes, cool flip no indentation pressure

。

80-100mj / square centimeter, 21 Table 6-8 light ladder frame (1-3kw      UV light, iodine gallium lamp mercury lamp 40-50 seconds), plating 100-120 、

Significant impact

mj / cm ²

0.8 ~ 1.2% sodium carbonate (Na2CO3) solution, 30 ± 2 ℃, 40 -

60 seconds of solution

Baked after

150-170 ℃, bake 20-30 minutes。

Etching

Acid or alkaline etching solution。

To film

5% sodium hydroxide (NaOH) solution, 50 ± 5 ℃ ,60-120sec